Testing was performed on a Grate Inlet Skimmer Box located at Longo Toyota in Ca.  The GISB was fitted with a # 3 Storm Boom.  ABN Environmental Labs of California performed the testing and provided the test data shown in the table below.

| Lab Test Results-Runoff Water Samples Collected At Longo Toyota Between Sept. 23, 2002 and Nov. 7, 2002 Test Results ABN Environmental Labs, South El Monte, CA |
| --- |
| Pollutant | Detection Limit mg/liter | Test 1No Filter mg/liter | Test 2After 1 week with filter; mg/liter | Test 3After 3 weeks with filter; mg/liter | Test 4After 5 weeks with filter; mg/liter |
| Oil & Grease | 2.70 | 198.00 | < 2.7 | 20.00 | 8.6 |
| Soap | 17.00 | 102.00 | 156.00 | 151.00 | 106.00 |
| Chromium | 0.05 | 0.47 | < 0.05 | < 0.05 | < 0.05 |
| Lead | 0.10 | 1.50 | 0.40 | < 0.10 | < 0.10 |
| Copper | 0.06 | 1.90 | 0.13 | 0.06 | 0.11 |
| Iron | 0.05 | 218.00 | 3.7 | 1.83 | 1.25 |
| Aluminum | 0.20 | 103.00 | 1.99 | 1.20 | 0.80 |
| Zinc | 0.10 | 13.70 | 1.10 | 0.34 | 0.76 |
| Nickel | 0.10 | 0.70 | 0.30 | < 0.10 | 0.16 |

# Text boxes

Ph               800-452-4435

Fax              615-822-9460

E-mail          jenhillconstr@msn.com

Website       WWW.JENHILL.COM